| AT-YR402Q |
| --- |
| In line with international | GB/T17493 E621T1-B3C |
| Equivalent | AWS A5.29 JIS Z3318 YF2CM-C |
| 熔敷金属主要成分(%) Typical composition of deposited metal |
| C | Mn | Si | S | P | Cr | Mo |  |  |  |
| 0.05-0.12 | ≤1.25 | ≤0.8 | ≤0.03 | ≤0.03 | 2-2.5 | 0.9-1.2 |  |  |  |
| 熔敷金属力学性能 Typical mechanical properties of deposited metal |
| Ｒm(MPa) | Ｒei(MPa) | A(%) |  |  |
| 620-760 | ≥540 | ≥17 |  |  |
| 用途 Function performance and application |
| For 2.25%Cr-1%Mo Heat Resistant Steel. |
| Current(A) | Diameter(mm) | 1.2 | 1.4 | 1.6 |
|  | F | 120-300 | 150-400 | 180-450 |
|  | V-up | 120-260 | 150-270 | 180-280 |
|  | V-down | 200-300 | 220-300 | 250-300 |
|  | H | 120-280 | 150-320 | 180-350 |
| 使用要点(Note) Use 100% CO2 gas CO2 mass flow should be controlled at 20-25l/min Out stick should be controlled in 15-25mm DC+ Proper preheating(160-190℃) and tempering after welding. |
| 参考价格(Price) | ／kg |
| 备注(Hit) |