| AT-YJ502NiJ |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| In line with international |  |  | GB/T17493 E501T1-9L |  |  |  |  |  |  |  |  |  |  |
| Equivalent |  |  | AWS 5.20 E71T1-9CJE71T1-12CJ JIS Z3313 YFW-C503R |  |  |  |  |  |  |  |  |  |  |
| 熔敷金属主要成分(%) Typical composition of deposited metal |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C | Mn | Si |  | S | P |  | Ni |  |  |  |  |  |  |
| ≤0.15 | ≤1.75 | ≤0.9 |  | ≤0.03 | ≤0.03 |  | ≤0.5 |  |  |  |  |  |  |
| 熔敷金属力学性能 Typical mechanical properties of deposited metal |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Ｒm(MPa) |  | Ｒei(MPa) |  |  | A(%) |  |  | Akv(J) -20℃ |  |  |  |  |  |
| ≥480 |  | ≥400 |  |  | ≥22 |  |  | ≥27 |  |  |  |  |  |
| 用途 Function performance and application |  |  |  |  |  |  |  |  |  |  |  |  |  |
| For mutual welding and corner welding of shipbuilding, ocean structures, bridges and tanks. |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Current(A) |  |  | Diameter(mm) |  |  | 1.2 |  |  |  |  |  |  |  |
|  |  |  | F |  |  | 120-300 |  |  |  |  |  |  |  |
|  |  |  | V-up |  |  | 120-260 |  |  |  |  |  |  |  |
|  |  |  | V-down |  |  | 200-300 |  |  |  |  |  |  |  |
|  |  |  | H |  |  | 120-280 |  |  |  |  |  |  |  |
| 使用要点(Note) - Use 100% CO2 gas。 - CO2 mass flow should be controlled at 20-25l/min - Out stick should be controlled in 15-25mm - DC+ |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 参考价格(Price) |  |  |  |  |  | ／kg |  |  |  |  |  |  |  |
| 备注(Hit) |  |  |  |  |  |  |  |  |  |  |  |  |  |