| AT-YJ502NiJ |
| --- |
| In line with international | GB/T17493 E501T1-9L |
| Equivalent | AWS 5.20 E71T1-9CJE71T1-12CJ JIS Z3313 YFW-C503R |
| 熔敷金属主要成分(%) Typical composition of deposited metal |
| C | Mn | Si | S | P | Ni |  |  |  |  |
| ≤0.15 | ≤1.75 | ≤0.9 | ≤0.03 | ≤0.03 | ≤0.5 |  |  |  |  |
| 熔敷金属力学性能 Typical mechanical properties of deposited metal |
| Ｒm(MPa) | Ｒei(MPa) | A(%) | Akv(J) -20℃ |  |
| ≥480 | ≥400 | ≥22 | ≥27 |  |
| 用途 Function performance and application |
| For mutual welding and corner welding of shipbuilding, ocean structures, bridges and tanks. |
| Current(A) | Diameter(mm) | 1.2 |  |  |
|  | F | 120-300 |  |  |
|  | V-up | 120-260 |  |  |
|  | V-down | 200-300 |  |  |
|  | H | 120-280 |  |  |
| 使用要点(Note) Use 100% CO2 gas。 CO2 mass flow should be controlled at 20-25l/min Out stick should be controlled in 15-25mm DC+ |
| 参考价格(Price) | ／kg |
| 备注(Hit) |