| AT-YJ501CrNiCu |
| --- |
| In line with international |  |
| Equivalent | JIS Z3320 YFA-50W |
| 熔敷金属主要成分(%) Typical composition of deposited metal |
| C | Mn | Si | S | P | Cr | Ni | Cu |  |  |
| ≤0.10 | ≤1.6 | ≤0.6 | ≤0.03 | ≤0.03 | 0.25-0.5 | 0.3-0.6 | 0.25-0.45 |  |  |
| 熔敷金属力学性能 Typical mechanical properties of deposited metal |
| Ｒm(MPa) | Ｒei(MPa) | A(%) | Akv(J) 0℃ |  |
| ≥500 | ≥410 | ≥22 | ≥47 |  |
| 用途 Function performance and application |
| For mutual welding and corner welding of shipbuilding, ocean structures, bridges and tanks. |
| Current(A) | Diameter(mm) | 1.2 | 1.4 | 1.6 |
|  | F | 120-300 | 150-400 | 180-450 |
|  | V-up | 120-260 | 150-270 | 180-280 |
|  | V-down | 200-300 | 200-300 | 180-350 |
|  | H | 120-280 | 150-350 | 180-400 |
| 使用要点(Note) Use 100% CO2 gas CO2 gas flow controlled at 20-25L/min Wire extension: 15-25mm |
| 参考价格(Price) | ／kg |
| 备注(Hit) |