| GL-YJ502Q |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| In line with international |  |  | GB/T10045 E501T-1/1M |  |  |  |  |  |  |  |  |  |  |
| Equivalent |  |  | AWS 5.20 E71T-1C/1M JIS Z3313 YFW-C50DR |  |  |  |  |  |  |  |  |  |  |
| 熔敷金属主要成分(%) Typical composition of deposited metal |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C | Si | Mn |  | S | P |  |  |  |  |  |  |  |  |
| ≤0.18 | ≤0.9 | ≤1.75 |  | ≤0.03 | ≤0.03 |  |  |  |  |  |  |  |  |
| 熔敷金属力学性能 Typical mechanical properties of deposited metal |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Ｒm(MPa) |  | Ｒei(MPa) |  |  | A(%) |  |  | Akv(J) -20℃ |  |  |  |  |  |
| ≥480 |  | ≥400 |  |  | ≥22 |  |  | ≥27 |  |  |  |  |  |
| 用途 Function performance and application |  |  |  |  |  |  |  |  |  |  |  |  |  |
| For mild steel and 490MPa high tensile steel, widely used in areas such as shipbuilding, bridges, constructions, heavy equipment and structural steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 参考焊接规范 Welding parameter |  |  | Diameter(mm) |  |  | 1.2 |  |  | 1.4 |  |  | 1.6 |  |
|  |  |  | F |  |  | 120-300 |  |  | 150-400 |  |  | 180-450 |  |
|  |  |  | V-up, OH |  |  | 120-260 |  |  | 150-270 |  |  | 180-280 |  |
|  |  |  | V-down |  |  | 200-300 |  |  | 220-300 |  |  | 250-300 |  |
|  |  |  | H |  |  | 120-280 |  |  | 150-320 |  |  | 180-350 |  |
| 使用要点(Note) - Use 100% CO2 gas - CO2 gas flow controlled at 20-25L/min - Wire extension: 15-25mm - DCRP(DC electrode position) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 参考价格(Price) |  |  |  |  |  | ／kg |  |  |  |  |  |  |  |
| 备注(Hit) |  |  |  |  |  |  |  |  |  |  |  |  |  |