| GL-YJ502Q |
| --- |
| In line with international | GB/T10045 E501T-1/1M |
| Equivalent | AWS 5.20 E71T-1C/1M JIS Z3313 YFW-C50DR |
| 熔敷金属主要成分(%) Typical composition of deposited metal |
| C | Si | Mn | S | P |  |  |  |  |  |
| ≤0.18 | ≤0.9 | ≤1.75 | ≤0.03 | ≤0.03 |  |  |  |  |  |
| 熔敷金属力学性能 Typical mechanical properties of deposited metal |
| Ｒm(MPa) | Ｒei(MPa) | A(%) | Akv(J) -20℃ |  |
| ≥480 | ≥400 | ≥22 | ≥27 |  |
| 用途 Function performance and application |
| For mild steel and 490MPa high tensile steel, widely used in areas such as shipbuilding, bridges, constructions, heavy equipment and structural steel |
| 参考焊接规范 Welding parameter | Diameter(mm) | 1.2 | 1.4 | 1.6 |
|  | F | 120-300 | 150-400 | 180-450 |
|  | V-up, OH | 120-260 | 150-270 | 180-280 |
|  | V-down | 200-300 | 220-300 | 250-300 |
|  | H | 120-280 | 150-320 | 180-350 |
| 使用要点(Note) Use 100% CO2 gas CO2 gas flow controlled at 20-25L/min Wire extension: 15-25mm DCRP(DC electrode position) |
| 参考价格(Price) | ／kg |
| 备注(Hit) |