| AT-Y2209 |
| --- |
| In line with international | GB/T17853 AWSA5.22 JISZ3323 E2209T1-1 |
| Equivalent | JIS Z3323 TS2209-FC1 |
| Typical composition of deposited metal (wt%) |
| C | Mn | Si | S | P | Cr | Mo | N | Ni |  |
| ≤0.04 | 0.5-2．5 | ≤1 | ≤0.03 | ≤0.04 | 21-24 | 2.5-4 | 0.08-0.2 | 7.5-10 |  |
| Typical mechanical properties of deposited metal |
| Ｒm(MPa) |  | A(%) |  |  |
| ≥690 |  | ≥25 |  |  |
| Function performance and application |
| For welding 22%Cr duplex stainless steel. |
| Welding Parameters | Diameter (mm) | 1.2 |  | 1.6 |
|  | Current (A) | 120-250 |  | 160-300 |
|  | CO2 Flow (L/min) | 20-25 |  | 20-25 |
| Note: The microstructure of deposited metal called “duplex” consisting of an austenitic - ferritic matrix, which increased deposited metal tensile strength, resistance to pitting corrosion and to stress corrosion cracking. |
| Price | Yuan／kg |