| AT-Y316LD |
| --- |
| In line with international | GB/T17853 AWSA5.22 JISZ3323 E316LT0-1 |
| Equivalent | JIS Z3323 TS316L-FC1 |
| Typical composition of deposited metal (wt%) |
| C | Mn | Si | S | P | Cr | Mo | Ni |  |  |
| ≤0.04 | 0.5-2．5 | ≤1 | ≤0.03 | ≤0.04 | 17-20 | 2-3 | 11-14 |  |  |
| Typical mechanical properties of deposited metal |
| Ｒm(MPa) |  | A(%) |  |  |
| ≥485 |  | ≥30 |  |  |
| Function performance and application |
| For cladding SUS316L. |
| Welding Parameters | Diameter (mm) | 1.2 |  | 1.6 |
|  | Current (A) | 120-250 |  | 160-300 |
|  | CO2 Flow (L/min) | 20-25 |  | 20-25 |
| Note: Austenitic in deposition contains a number of ferrite which results less cracking and flaw free welding zone will be acquired. Besides with ability of corrosion resistance in diluted sulphuric acid and heat resistance because of Mo. |
| Price | Yuan／kg |