| AT-Y347LD |
| --- |
| In line with international | GB/T17853 AWSA5.22 JISZ3323 E347LT0-1 |
| Equivalent | JIS Z3323 TS347L-FC1 |
| Typical composition of deposited metal (wt%) |
| C | Mn | Si | S | P | Cr | Mo | Ni | Nb |  |
| ≤0.04 | 0.5-2．5 | ≤1 | ≤0.03 | ≤0.04 | 18-21 | ≤0.5 | 9-11 | 8×C-1.0 |  |
| Typical mechanical properties of deposited metal |
| Ｒm(MPa) |  | A(%) |  |  |
| ≥520 |  | ≥25 |  |  |
| Function performance and application |
| For welding petrochemical, pressure vessel, food machine and medical apparatus. |
| Welding Parameters | Diameter (mm) | 1.2 |  | 1.6 |
|  | Current (A) | 120-250 |  | 160-300 |
|  | CO2 Flow (L/min) | 20-25 |  | 20-25 |
| Note: Be able to resist intercrystalline corrosion caused by separating carbide because of Nb. |
| Price | Yuan／kg |