| AT-YJ70MC |
| --- |
| In line with international | GB/T10045 E500T-1C |
| Equivalent | AWS 5.20 E70T-1C |
| Typical composition of deposited metal (wt%) |
| C | Mn | Si | S | P |  |  |  |  |  |
| ≤0.18 | ≤1.75 | ≤0.9 | ≤0.03 | ≤0.03 |  |  |  |  |  |
| Typical mechanical properties of deposited metal |
| Ｒm(MPa) | Ｒei(MPa) | A(%) | Akv(J) -20℃ |  |
| ≥500 | ≥410 | ≥22 | ≥47 |  |
| Function performance and application |
| Metal core FCW for auto and semi-auto welding, single-bead and multi-pass welding on the application realms such as shipbuilding, bridge and steel structure fabricating. |
| .Welding Parameters | Diameter (mm) | 1.2 | 1.4 | 1.6 |
|  | Current (A) | 150-350 | 170-400 | 200-450 |
|  | CO2 Flow (L/min) | 180-350 | 200-350 | 260-400 |
| Note: Use 100% CO2 gas CO2 gas flow controlled at 20-25L/min Wire extension: 15-25mm. DCRP(DC electrode position) |
| Price | Yuan／kg |