| AT-YJ70MC |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| In line with international |  |  | GB/T10045 E500T-1C |  |  |  |  |  |  |  |  |  |  |
| Equivalent |  |  | AWS 5.20 E70T-1C |  |  |  |  |  |  |  |  |  |  |
| Typical composition of deposited metal (wt%) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C | Mn | Si |  | S | P |  |  |  |  |  |  |  |  |
| ≤0.18 | ≤1.75 | ≤0.9 |  | ≤0.03 | ≤0.03 |  |  |  |  |  |  |  |  |
| Typical mechanical properties of deposited metal |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Ｒm(MPa) |  | Ｒei(MPa) |  |  | A(%) |  |  | Akv(J) -20℃ |  |  |  |  |  |
| ≥500 |  | ≥410 |  |  | ≥22 |  |  | ≥47 |  |  |  |  |  |
| Function performance and application |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Metal core FCW for auto and semi-auto welding, single-bead and multi-pass welding on the application realms such as shipbuilding, bridge and steel structure fabricating. |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .Welding Parameters |  |  | Diameter (mm) |  |  | 1.2 |  |  | 1.4 |  |  | 1.6 |  |
|  |  |  | Current (A) |  |  | 150-350 |  |  | 170-400 |  |  | 200-450 |  |
|  |  |  | CO2 Flow (L/min) |  |  | 180-350 |  |  | 200-350 |  |  | 260-400 |  |
| Note: - Use 100% CO2 gas - CO2 gas flow controlled at 20-25L/min - Wire extension: 15-25mm. - DCRP(DC electrode position) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Price |  |  |  |  |  | Yuan／kg |  |  |  |  |  |  |  |