| AT-X80 |
| --- |
| In line with international | GB/T17493 E551T8-Ni2 AWSA5.29 E81T1-Ni2J |
| Equivalent |  |
| Typical composition of deposited metal (wt%) |
| C | Mn | Si | S | P | Al | Ni |  |  |  |
| 0.05 | 1.45 | 0.1 | 0.03 | 0.01 | 1 | 2.5 |  |  |  |
| Typical mechanical properties of deposited metal |
| Ｒm(MPa) | Ｒei(MPa) | A(%) | Akv(J) -20℃ |  |
| 690 | 600 | 19 | 100 |  |
| Function performance and application |
| For self-shielding circumferential welding X80 Grade pipeline steel in pipeline ladying. |
| Welding Parameters | Diameter (mm) | 2.0 |  |  |
|  | F | 160-300 |  |  |
|  | V-up, OH | 120-220 |  |  |
|  | V-down | 160-260 |  |  |
|  | H | 120-280 |  |  |
| Note: CO2 gas flow controlled at 20-25L/min DCRP(DC electrode position) |
| Price |  |