| AT-YJ621K2 |
| --- |
| In line with international | GB/T17493 E621T1-K2C |
| Equivalent | AWS 5.29 E91T1-K2 JISZ3313 YFW-C602R |
| Typical composition of deposited metal (wt%) |
| C | Mn | Si | S | P | Ni | Mo |  |  |  |
| ≤0.15 | ≤0.5-1.75 | ≤0.8 | ≤0.03 | ≤0.03 | 1-2 | ≤0.35 |  |  |  |
| Typical mechanical properties of deposited metal |
| Ｒm(MPa) | Ｒei(MPa) | A(%) | Akv(J) -20℃ |  |
| 620-760 | ≥540 | ≥17 | ≥27 |  |
| Function performance and application |
| For welding 620MP Grade high tensile strength steel. |
| Welding Parameters | Diameter (mm) | 1.2 |  |  |
|  | F | 120-300 |  |  |
|  | V-up, OH | 120-260 |  |  |
|  | V-down | 200-300 |  |  |
|  | H | 120-280 |  |  |
| Note: Use 100% CO2 gas CO2 gas flow controlled at 20-25L/min Wire extension: 15-25mm. DCRP(DC electrode position) According to the different conditions, the base metal should be preheated in 135-165℃. |
| Price | Price |